## The Iron ‐ Iron Carbide (Fe‐Fe3C) Phase Diagram

Reactions

Peritectic L    

at T=1493oC and 0.18wt%C

Eutectic L    Fe3C

at T=1147oC and 4.3wt%C

## Phases Present

L

 austenite Fcc structure Non‐magnetic ductile

 ferrite delta Bcc structure Paramagnetic

Eutectoid     Fe C

3

at T=727oC and 0.77wt%C

Fe3C cementite Orthorhombic Hard, brittle

 ferrite Bcc structure Ferromagnetic Fairly ductile

Max. solubility of C in ferrite=0.022% in austenite=2.11%

## Phases in Fe–Fe3C Phase Diagram

- ‐ferrite ‐ solid solution of C in BCC Fe

  - Stable form of iron at room temperature.

  - Transforms to FCC g‐austenite at 912 C

- ‐austenite ‐ solid solution of C in FCC Fe

  - Transforms to BCC ‐ferrite at 1395 C

  - Is not stable below the eutectic temperature (727  C) unless cooled rapidly.

- ‐ferrite solid solution of C in BCC Fe

  - It is stable only at T, >1394 C. It melts at 1538 C

- Fe3C (iron carbide or cementite)

  - This intermetallic compound is metastable at room T. It decomposes (very slowly, within several years) into ‐Fe and C (graphite) at 650 ‐ 700 C

- Fe‐C liquid solution

## Comments on Fe–Fe3C system

C is an interstitial impurity in Fe. It forms a solid solution with  

 phases of iron

Maximum solubility in BCC ‐ferrite is 0.022 wt% at 727 C. BCC: relatively small interstitial positions

Maximum solubility in FCC austenite is 2.14 wt% at 1147 C ‐ FCC has larger interstitial positions

Mechanical properties: Cementite (Fe3C is hard and brittle: strengthens steels). Mechanical properties also depend on microstructure: how ferrite and cementite are mixed.

Magnetic properties:  ‐ferrite is magnetic below 768 C, austenite is non‐magnetic

## Classification.

Three types of ferrous alloys:

Iron: < 0.008 wt % C in ‐ferrite at room T Steels: 0.008 ‐ 2.14 wt % C (usually < 1 wt % )

‐ferrite + Fe3C at room T

Cast iron: 2.14 ‐ 6.7 wt % (usually < 4.5 wt %)

3

1

3

# Eutectoid steel

Microstructure of eutectoid steel

Alloy of eutectoid composition (0.76 wt % C) is cooled slowly: forms

pearlite, layered structure of two phases:	‐ferrite and cementite (Fe3C)

Mechanically, pearlite has properties

intermediate to soft, ductile ferrite and hard, brittle cementite.

# Hypoeutectoid steel

Hypoeutectoid alloys

contain proeutectoid ferrite (formed above the eutectoid temperature) plus the eutectoid perlite that contain eutectoid ferrite and cementite.

# Hypereutectoid steel

Hypereutectoid alloys contain proeutectoid cementite (formed above the eutectoid temperature) plus perlite that contain eutectoid ferrite and cementite.